## Slide 1
Samarium-Cobalt Based Magnets
Advanced Permanent Magnet Technology for Engineering Applications
Comprehensive Research & Industry Applications • February 2026

## Slide 2
What are Samarium-Cobalt Magnets?
Rare-earth permanent magnets composed of samarium and cobalt alloys, discovered in the early 1960s by Karl Strnat and Alden Ray. These were the first commercially viable rare-earth magnets.
SmCo₅ (Series 1:5)
• First developed (early 1960s)
• Energy: 15-24 MGOe
• Max temp: 250°C
• No iron content
• Excellent corrosion resistance
Sm₂Co₁₇ (Series 2:17)
• Modern formulation (1980s)
• Energy: 20-33 MGOe
• Max temp: 350°C
• Contains Fe, Cu, Zr traces
• Industry standard today

## Slide 3
Permanent Magnet Materials Comparison
Property | SmCo | NdFeB | Alnico | Ferrite
Energy (MGOe) | 16-33 | 35-52 | 1.5-10 | 3.5-5
Max Temp | 250-350°C | 80-230°C | 450-550°C | 250-300°C
Temp Coeff | -0.035%/°C | -0.11%/°C | -0.02%/°C | -0.18%/°C
Corrosion | Excellent | Poor (coating) | Good | Excellent
Cost | Very High | High | Medium | Low
Green = Superior | Yellow = Moderate | Selection depends on application requirements

## Slide 4
Why Choose SmCo for Critical Applications?
Temperature Stability
3× better coefficient (-0.035%/°C vs -0.11%/°C for NdFeB)
High Operating Temp
Up to 350°C continuous (NdFeB fails at 230°C)
Corrosion Resistance
No coating required, ideal for marine & medical use
Demagnetization Resistance
Hci: 8-30 kOe ensures stability under opposing fields

## Slide 5
Halbach Array Configuration
Discovered by Klaus Halbach (1980s): Spatially rotating magnetization pattern that concentrates field on one side while canceling on the opposite side
Standard Radial Array
• Equal field both sides
• Wasted field energy
• Enhancement: 1.0×
Halbach Array
• 2× stronger on working side
• 40-50% field boost
• Enhancement: 1.4-1.5×

## Slide 6
Temperature Performance Analysis
-20°C
100.7%
Arctic conditions
25°C
100%
Reference point
150°C
95.6%
NdFeB fails here
250°C
91.2%
SmCo₅ max
350°C
87.5%
Sm₂Co₁₇ max

## Slide 7
Long-Term Degradation Analysis
Cumulative effects over 10-year service life at 70°C:
Magnet flux loss
0.35 T
→
0.322 T
-8%
Air gap increase
3.0 mm
→
3.3 mm
+10%
Combined effect
100%
→
77%
-23%
Result: Terminal velocity increases from 1.30 m/s to 1.85 m/s (10-year service interval required)

## Slide 8
Velocity Increase Over Service Life
Chart: 
| Year 0 | Year 2 | Year 4 | Year 6 | Year 8 | Year 10
Terminal Velocity | 1.3 | 1.45 | 1.6 | 1.75 | 1.91 | 2.07
Safety Limit | 2 | 2 | 2 | 2 | 2 | 2

## Slide 9
Maintenance Strategy
Annual (Years 1-9)
• Visual inspection
• Drop test verification
• Rope replacement
10-Year Major Service
• Field strength measurement
• Air gap verification
• Replace magnets/bearings
Decision Tree:
✓ Flux ≥85% & gap ≤3.5mm → Continue service
⚠ Flux <85% OR gap >3.5mm → Replace components
✗ Severe degradation → Decommission unit

## Slide 10
Industrial Applications Portfolio
✈️ Aerospace
Aircraft systems, satellites, missiles
🏥 Medical
MRI coils, surgical tools, implants
🚗 Automotive
Sensors, power steering, EV motors
⚡ Energy
Wind turbines, generators, flywheels
🏭 Industrial
Motors, couplings, magnetic bearings
📡 Electronics
Microwave tubes, particle accelerators

## Slide 11
Eddy Current Braking Applications
🚆 Rail
High-speed trains, metro systems, maglev
🎢 Amusement
Roller coasters, drop towers, zip lines
🏭 Industrial
Power tools, dynamometers, cranes
⚡ Power Gen
Wind turbines, generators, flywheels
🏃 Fitness
Ellipticals, bikes, rowing machines
🧗 Safety
Auto-belays, descent devices, rope courses

## Slide 12
Built-In Safety Features
✓
Self-Regulating
Velocity-proportional braking automatically increases with speed
✓
No Wear Parts
Electromagnetic operation eliminates friction surfaces and fluid seals
✓
Temperature Stable
SmCo maintains 87%+ performance from -273°C to +350°C
✓
Predictable Degradation
Gradual velocity increase (0.077 m/s/year) allows proactive maintenance
✓
Passive Operation
No electrical power required - always ready, never battery failure

## Slide 13
Critical Design Parameters
Air Gap
B² / δ³
Cubic power - most critical
Very High
Magnetic Flux
B²
Square relationship
High
Conductivity
σ
Linear relationship
Medium
Disc Thickness
t
Linear with penetration
Medium
Air gap tolerance (±0.5mm) is the most sensitive parameter affecting performance

## Slide 14
Energy Dissipation & Thermal Management
Energy Calculation
Total energy: 35,316 J
Average power: 1,083 W
Temperature Rise
Disc mass: 1.6 kg
Specific heat: 900 J/(kg·°C)
ΔT = 20.5°C
Start: 25°C → Final: 66°C
(Safe for handling)
SmCo magnets (rated to 350°C) experience NO thermal stress at 66°C operating temperature

## Slide 15
SmCo vs. Alternative Technologies
Technology | Advantages | Disadvantages
SmCo Eddy Current | No wear 10yr service Temp stable | High initial cost 10yr maintenance
Friction Brakes | Low cost Simple | Brake fade >150°C Frequent replacement Sudden failure
Hydraulic Dampers | Smooth Adjustable | Seal failures Temp sensitive Fluid maintenance
NdFeB Eddy Current | Higher strength Lower cost | Poor temp stability Corrosion prone Coating required

## Slide 16
SmCo Manufacturing Process
1
Melting
Alloy at 1400°C
2
Milling
Powder 3-5 μm
3
Pressing
Magnetic alignment
4
Sintering
1100-1250°C
5
Heat Treat
700-900°C
6
Machining
Diamond tools
7
Magnetize
>3 Tesla field
8
Testing
QC verification

## Slide 17
Key Takeaways
1
SmCo offers unmatched temperature stability (-0.035%/°C) for mission-critical applications
2
Halbach arrays provide 40% field enhancement, maximizing braking effectiveness
3
Predictable degradation enables proactive 10-year maintenance scheduling
4
Self-regulating velocity-dependent braking ensures inherent safety
5
Validated through analytical modeling and 3D finite element simulation
6
20+ year service life with proper maintenance protocols

## Slide 18
Global Market & Growth Potential
SmCo magnets represent 2-3% of global permanent magnet market (growing 8-10% annually)
Aerospace & Defense
Market Share: 35%
Growth: +12%/yr
Value: $580M
Automotive (Premium EV)
Market Share: 25%
Growth: +15%/yr
Value: $415M
Medical Devices
Market Share: 18%
Growth: +9%/yr
Value: $298M
Industrial Equipment
Market Share: 15%
Growth: +7%/yr
Value: $249M
Consumer Electronics
Market Share: 7%
Growth: +5%/yr
Value: $116M
Total addressable market: ~$1.66B (2026) | Projected: $2.8B by 2030

## Slide 19
Challenges & Limitations
High Material Cost
SmCo 3-5× cost of NdFeB
→ Justify with TCO analysis for critical applications
Brittleness
Prone to chipping, difficult machining
→ Diamond tools, careful handling, protective coatings
Supply Chain
Rare earth dependency (China 80%+ production)
→ Diversify sources, recycling programs, strategic reserves
Assembly Complexity
Halbach arrays require precision alignment
→ Automated assembly jigs, QC protocols, tolerance analysis
Demagnetization Risk
Improper handling can damage magnets
→ Training, handling procedures, storage guidelines

## Slide 20
Conclusions & Future Outlook
✓ SmCo magnets enable applications impossible with other magnetic materials
✓ Superior temperature stability and corrosion resistance justify premium cost
✓ Halbach arrays maximize performance in eddy current systems
✓ Predictable degradation enables 20+ year service life with scheduled maintenance
✓ Growing market driven by aerospace, automotive, and medical applications
From cryogenic research to high-temperature aerospace: SmCo magnets enable the impossible